## Slide 1
20120015 Ankam Ravi Varma
20120024 Kiran Kumar Challa
20120062 Nimmaka Meghana
20120103 Vallepu Prabhu Das
19120062 Panjala Samanvitha
Supervised By:
Dr. Naga Sruthi Neelam
Process optimization in FSW of two similar γ-TiAl alloys using ML approach
Department of Metallurgical and Materials Engineering
National Institute of Technology
Raipur – 492 010
Project Viva

## Slide 2: Contents
INTRODUCTION
    TiAl alloys
    Friction stir welding
    Machine Learning
  OBJECTIVE
  METHODOLOGY
  RESULTS AND DISCUSSIONS
  SUMMARY & CONCLUSION

## Slide 3
Gamma TiAl based alloy Concepts
g-TiAl alloys possess low specific weight (r=3.9 gm/cm3)-leads to substantial weight saving
High Elastic Stiffness (E=170 GPa)
Good oxidation resistance up to 750°C
High tensile strength and fatigue strength
Why g-TiAl alloys?
Weight reduction
Substantial reduction in CO2 and NOx emission.
Substantial noise and cost reduction.
g-TiAl alloys:
γ-Ti-46.5Al-5Nb-2Mo-0.3B
lamellar
a2+g
b/B2

## Slide 4
Blades
Courtesy: GE aviation
Applications:
Aerospace and automotive applications

## Slide 5
Friction Stir Welding (FSW):
What is FSW?
  Solid state joining process
  A non-consumable rotating tool is used to generate frictional heat between the tool and the materials leading to material mixing for a metallurgical and mechanical bonding at the interface
WHY?
  Economic, effective and relatively productive
  No requirement of vacuum, shield gas, filler materials etc.

## Slide 6
Current Status of Work
Inherent brittleness; high dependence of properties on structure and composition of γ-TiAl alloys
Challenging to control the metallurgy of the material and to prevent cracking during welding
Joining Method | Limitation
Friction stir welding | Solid state cracking
Diffusion bonding | Brittle α2 phase along the bond line degrading the mechanical properties
Laser/Electron beam | High thermal stresses; α-γ phase transformation
Use of interlayers | Compromising the composition of the material
Careful optimization of welding parameters, preheating to 700–800 °C, etc.
Joining of Gamma-based Titanium Aluminides – A Review: A. S. Ramos et.al., Materials Science Forum Vols. 514-516 (2006) pp 483-489
The joining of gamma titanium aluminides via the powder interlayer bonding method; Davies, P.D., Davies, H.M., Watkins, I. et al.; Int J Adv Manuf Technol 109, 2049–2054 (2020)

## Slide 7: Machine Learning
Machine learning is like teaching computers to learn from data and make decisions without being explicitly programmed for each task.
It's about creating algorithms that can recognize patterns and make predictions or decisions based on examples or experiences.

## Slide 8: Machine Learning in FSW
Machine learning is increasingly being used in various aspects of Friction Stir Welding (FSW) to enhance the process, improve quality control, and optimize parameters.
Here are some ways in which machine learning is applied to FSW:
  Quality Control
  Process Optimization
  Anomaly Detection
  Predictive Maintenance
  Material Selection
  Weld Parameter Optimization
  Simulation and Design.
  Data Analysis.
Y. Du, T. Mukherjee, P. Mitra, T. DebRoy, Machine learning based hierarchy of causative variables for tool failure in friction stir welding, Acta Materialia, Volume 192, 2020, Pages 67-77,

## Slide 9
Optimization of FSW parameters to obtain a defect free joint of γ-Ti-46.5Al-5Nb-2Mo-0.3B alloy using Machine learning
  To generate sufficient data set for Machine learning process
  Optimization of process parameters using various ML algorithms – to reduce the experimental trails in obtaining a defect free joint
Research Objectives:

## Slide 10: Process parameters of FSW for ML:
Rotation Speed
Traverse Speed
Tool Geometry
Plunge Depth
Friction Time
Upset Pressure
Friction Pressure
Tilt angle
Independent Variable.
  Rotation Speed
  Friction Time
  Upset Pressure
  Friction Pressure
  Tilt angle
And Output Variable
  Tensile Strength
Y. Du, T. Mukherjee, P. Mitra, T. DebRoy, Machine learning based hierarchy of causative variables for tool failure in friction stir welding, Acta Materialia, Volume 192, 2020, Pages 67-77,

## Slide 11: Methodology
DATA COLLECTION
  Assembled a dataset by reviewing literature and extracting sample data from research journals.
  The defined ranges of each parameter were sourced from these journals.
  Tensile Strength ranges from 120-450 MPa
PROCESS PARAMETER | RANGE
Rotational Speed | 2000-2500 rpm
Friction Time | 30-50 sec
Upset Pressure | 300-460 MPa
Friction Pressure | 130-170 MPa
Tilt Angle | 1- 3 ⁰
Microstructure and Mechanical Properties of Ti-48Al-2Cr-2Nb Manufactured Via Electron Beam Melting DO - 10.1002/9781119296126.ch223
Joining Technology of gamma-TiAl Alloys By Sonia Luisa dos Santos Simoes, Filomena Maria da Conceicao Viana, Manuel Fernando Goncalves Vieira

## Slide 12: Methodology
2) IMPLEMENTATION OF MACHINE LEARNING ALGORITHMS
  Importing the python libraries
  Loading the FSW data set
  Exploratory data analysis on FSW data set
  Splitting the data set
  Implementation of ML algorithms
  Evaluation of ML Models
Y. Du, T. Mukherjee, P. Mitra, T. DebRoy, Machine learning based hierarchy of causative variables for tool failure in friction stir welding, Acta Materialia, Volume 192, 2020, Pages 67-77,

## Slide 13
Exploratory Data Analysis

## Slide 14
It is observed that the Rotational Speed (RPM) has the highest influence on the nature of TS (MPa).
Tilt Angle does not influence much on the nature of TS (MPa).
Feature Importance

## Slide 15
Correlation between the Variables

## Slide 16: Results and Discussion
Decision Tree Algorithm
Decision Tree is a greed-based non-parametric machine learning algorithm used to predict the target variable, i.e., Tensile Strength.
The Decision Tree model performed well, explaining 86.5% of the outcome's variation (R-squared) and showing small prediction errors (MAE) with a value of 28.189.

## Slide 17: Decision Tree Architecture

## Slide 18
Random Forest algorithm is a supervised machine learning algorithm constituted from decision trees.
The predicted output is generated by the outcome resulted from the decision trees by taking the mean or average of the output yielded from the individual decision trees.
Random Forest Algorithm
The Random Forest model did well, explaining 84.5% of the result, and it made accurate predictions with a small error (MSE: 34.481)

## Slide 19: Architecture of Random Forest Algorithm

## Slide 20
Gradient Boosting algorithm is an ensemble model that combines the weal learners or weak predictive models to predict the continuous value further.
It is observed that the Gradient Boosting Algorithm results the best fit by yielding the highest value of 0.890 in comparison to the other two algorithms.
Gradient Boosting Algorithm

## Slide 21
Optimized Parameters
Rotational Speed | Friction Time | Upset Pressure | Friction Pressure | Tilt Angle | Tensile Strength
2309 | 35 | 412 | 159 | 1 | 418(MAX)
2480 | 31 | 319 | 137 | 1 | 127(MIN)
Rotational Speed- 2000 rpm, Friction Time – 42 s, Upset Pressure-411 MPa, Friction Pressure-139 MPa, Tilt Angle- 2°
Predicted Output – 160.17 MPa
Actual Output – 157 MPa
Custom Inputs -

## Slide 22
Data set required for ML process is obtained from the literature and expanded using various mathematical algorithms
Supervised machine learning regression-based algorithms, including Decision Trees, Gradient Boosting Algorithm, and Random Forest Algorithm, using Python programming were implemented
Highest and least tensile strength of 418 MPa and 127 MPa respectively was achieved for the alloy γ-Ti-46.5Al-5Nb-2Mo-0.3B under specific parameter settings
These results can be taken as a guideline and be validated with the experimental setup for joining similar γ-Ti-46.5Al-5Nb-2Mo-0.3B alloys using FSW to obtain defect free joints
Summary and Conclusions

## Slide 23
Thank you